TRIBHUVAN UNIVERSITY

INSTITUTE OF ENGINEERING

PULCHOWK CAMPUS

dEPARTMENT OF CIVIL ENGINEERING

M. Sc. Program in Structural Engineering

### Thesis No.: SS00125

NONLINEAR DYNAMIC RESPONSE OF REINFORCED CONCRETE COVERED CANAL UNDER STRONG GROUND MOTIONS

MINESH RATNA TAMRAKAR

April 2009

TRIBHUVAN UNIVERSITY

INSTITUTE OF ENGINEERING

PULCHOWK CAMPUS

dEPARTMENT OF CIVIL ENGINEERING

# M. Sc. Program in Structural Engineering

### Thesis No.: SS00125

NONLINEAR DYNAMIC RESPONSE OF REINFORCED CONCRETE COVERED CANAL UNDER STRONG GROUND MOTIONS

A Thesis Report submitted by

MINESH RATNA TAMRAKAR

In the partial fulfillment of the requirements for the degree

Of

MASTER OF SCIENCE

IN

STRUCTURAL ENGINEERING

April 2009

#### CERTIFICATE

This is to certify that the work contained in this thesis entitled Nonlinear Dynamic Response of Reinforced Concrete Covered Canal under strong ground motions, in partial fulfillment of the requirements for the degree of Master of Science in Structural Engineering, as a record of research work, has been carried out by Mr. Minesh Ratna Tamrakar (063/MSS/f/106) under my supervision and guidance in the Institute of Engineering, Pulchowk Campus, Lalitpur, Nepal. The work embodied in this thesis has not been submitted elsewhere for a degree.

…………………………………

Dr. Roshan Tuladhar

(Department of Civil Engineering)

Institute of Engineering

Pulchowk Campus

Lalitpur, Nepal.

#### ACKNOWLEDGEMENT

Research is a process of advancement of knowledge for the benefit of society and mankind. It is the greatest contribution that a person can give to the society and mankind. To get an opportunity to do research is actually a great honor one can have. A feel of satisfaction that is achieved while carrying out a research work is almost impossible to express in words; can only be felt.

The research work presented in this thesis was conducted at the department of civil engineering, Pulchowk campus, Institute of Engineering, Tribhuvan University, Lalitpur, Nepal. The thesis was carried out under the supervision of Dr. Roshan Tuladhar.

First of all, I would like to express sincere gratitude to my supervisor Dr. Roshan Tuladhar for his valuable advice, guidance and kind support during the entire research work.

I would also like to thank all the course coordinators of the Structural engineering program who trained me and made me capable of undertaking the research work.

Finally, I would like to thank my family members and all of my friends for their love, continuous support and encouragement during my entire study period.

Minesh Ratna Tamrakar

April 2009			Lalitpur, Nepal

#### ABSTRACT

Underground structures have been considered to be relatively safer during the event of earthquakes. This belief has continued to make its roots in the engineers’ mind until the 1995 Hanshin-Awaji earthquake (Kobe earthquake). The Kobe earthquake witnessed severe damage and complete collapse of several subway stations belonging to Kobe metropolitan subway line. Similarly, recent 1999 Chi-Chi earthquake and 1999 Kocaeli earthquake also witnessed severe damages. These events have raised the serious concerns regarding the safety of the underground structures during earthquake. In Nepal, some of the underground structures have been constructed and some are underway to construction. In light of the damages that occurred in underground structures in recent times around the various parts of the world, detailed investigation of the seismic performance of the structures that is currently underway construction and the structures that are to be constructed in future have to be made. It is intended to study the performance of the to be constructed three-chambered reinforced concrete Covered Canal under severe ground motion due to earthquakes, which is a component of SIKTA Irrigation project. For accessing the performance of the covered canal, six different conditions of water levels have been considered. The soil investigation has not been carried out in the region where this structure is going to be constructed. So, for the purpose of the research, soil database of the head works have been utilized. The analysis showed that the covered canal is safer in the event of earthquakes. But, as the soil data used in the analysis is not the one found at the covered canal vicinity, it could not be generalized that the structure is safe in the event of earthquakes. So, it is deemed to be necessary to access the performance of the covered canal in various kinds of multi layered soil profiles. For this purpose, eleven models have been developed. These eleven models are grouped into three sets. First set consists of the three models having only one layer of soil each. Second set consists of six models with thickness and number of soil layers identical to original base case and varying the profiles by combination of soil properties. Third set consists of two models apart from base case with soil properties and number of soil layers identical to the base case and varying the thickness of the soil layers. These studies have revealed that the different types of soil profiles have got profound effect on the performance of the underground structures.

tABLE OF CONTENT

COPYRIGHT	I

CERTIFICATE	II

ACKNOWLEDGEMENT	III

ABSTRACT	IV

List of Symbols used	V

List of Abbreviations used	V

List of Figures	VIII

List of Tables	IX

1	INTRODUCTION	1

1.1	Background and Motivation	1

1.2	Problems and Issues	3

1.3	Objectives and Scope of the study	4

1.3.1	Overall Objective	4

1.3.2	Specific Objectives	4

1.4	Methodology	4

1.5	Organization of the thesis	5

2	LITERATURE REVIEW	7

2.1	Soil - Structure Interaction	7

2.2	Seismic Bed Rock	7

2.3	Finite Element Modeling Issues	8

2.4	The physics of the Symmetric and anti symmetric lateral boundary condition	11

2.5	Soil-Structure Interface	12

2.6	Joint Element	12

2.7	Past Research on Underground RC Structures	14

2.8	Past Research on Finite Element Modeling	20

3	DYNAMIC FEM ANALYSIS OF RC – SOIL SYSTEM	26

3.1	The Computational Simulation Tool: WCOMD	26

3.2	Modeling of RC-Soil System	29

4	NUMERICAL ANALYSIS	31

4.1	Geological Profile at Sikta Irrigation Project	31

4.2	Geometry of Covered Canal	32

4.3	Layout of Reinforcements	32

4.4	Soil Profile used in Computation	33

4.5	Material Properties	34

4.5.1	Structural Material Properties	34

4.5.2	Soil Material Properties	34

4.6	Far Field Boundary Condition	35

4.7	Input Earthquake Wave motion	36

4.8	Water Pressure Loads	37

4.9	Finite Element Mesh	37

4.10	Analysis Cases	39

4.10.1	Six Conditions of Water Level	39

4.10.2	Eleven Cases of Soil Profiles	39

4.10.3	Designation of Models	42

5	RESULTS AND DISCUSSION	44

5.1	General	44

5.2	Mean Inelastic Strain	44

5.3	Damage Criteria	45

5.4	Results of Water Cases	46

5.4.1	Mean Inelastic Strain	46

5.4.2	Damage Level	50

5.4.3	Deformation, Crack Pattern and Yield Locations	50

5.4.4	Variation of Stress and Strain in time domain	52

5.5	Results of Soil Profile Cases	53

5.5.1	Mean Inelastic Strain	54

5.5.2	Comparison of Peak Mean inelastic strain	62

5.5.3	Damage Level	62

5.5.4	Peak acceleration	64

5.5.5	Relative displacement	64

5.5.6	Variation of Stress and Strain in Time domain	65

6	CONCLUSIONS	79

7	RECOMMENDATIONS FOR FUTURE WORKS	81

8	REFERENCES	82

##### List of Tables

Table 1	Soil profile and its characteristics					34

Table 2	Designation and details of seventeen FE models			43

Table 3	Grouping of eleven soil profiles results into three sets		54

##### List of Figures

Figure 2.1	Soil-Structure Interaction Model					9

Figure 2.2	Mixed Artificial Boundary condition attached to the main mesh	10

Figure 2.3	Nature of Pulse							11

Figure 2.4	Ideal constitutive relationship of Joint element			13

Figure 2.5	Constitutive relationship of Joint element used in numerical

Analysis								13

Figure 2.6 	Finite element model used in soil-structure numerical analysis

of Daikai subway station						21

Figure 2.7	Finite element model used for analysis of strain

transmitting characteristics of underground structure			21

Figure 2.8	Finite element model used for soil-structure interaction

analysis of large underground structure in liquefiable soil		22

Figure 2.9	Finite element mesh used for investigating the collapse

of Daikai subway station						23

Figure 3.1	UC-win / mesh window						27

Figure 3.2	UC-win / WCOMD window						27

Figure 3.3	Constitutive relationship for RC / Soil interface			28

Figure 4.1	Geometry of Covered canal						32

Figure 4.2	Reinforcement details in Covered canal				32

Figure 4.3	Soil profile considered in computation (Base Case)			33

Figure 4.4	Mixed Artificial Boundary condition					35

Figure 4.5	Input Earthquake Wave						36

Figure 4.6	Finite Element Mesh							37

Figure 4.7	Overlapping plates at the lateral boundary				38

Figure 4.8	Enlarged view of finite element mesh of Covered canal 		38

Figure 4.9	Six conditions of water level						39

Figure 4.10a	Soil profile with six possible combinations of soil properties

A, B and C								40

Figure 4.10b	Soil profile having only single layer of soil A or B or C of total

height of soil domain							41

Figure 4.10c	Soil profile with almost equal thickness soil layers with soil

Properties identical to base case					41

Figure 4.10d	Soil properties with smaller middle layer sandwiched between

two large layers having soil properties identical to base case	42

Figure 5.1	Mean inelastic strain in time domain for various water cases	46

Figure 5.2	Damage locations in the structure					50

Figure 5.3	Maximum Deformation Profile					51

Figure 5.4	Crack pattern at maximum deformation				51

Figure 5.5	Yield locations in the structure					52

Figure 5.6 (a)	Element 499 along with gauss point 31				52

Figure 5.6 (b)	Peak tensile strains for various water cases				53

Figure 5.7	Mean inelastic strain in time domain for soil profiles

consisting of single layer soil						55

Figure 5.8	Mean inelastic strains in time domain for soil profiles

consisting of combination of soil properties A, B and C		57

Figure 5.9a	Plot of mean inelastic strain of soil profiles ABC with soil

layers of equal thickness						60

Figure 5.9b	Plot of mean inelastic strain of soil profiles ABC with middle

layer of small thickness						61

Figure 5.10	Peak damage for soil profile CC_SP_ABC_MLST			63

Figure 5.11	Residual damage for soil profile CC_SP_ABC_MLST		63

Figure 5.12	Peak acceleration at the top and bottom of the structure		64

Figure 5.13	Relative displacement between the top and bottom of the

Structure								65

Figure 5.14	Element 465 along with gauss point 32				65

Figure 5.15	Variation of stress XX in time domain for various soil profiles	67

Figure 5.16	Variation of stress YY in time domain for various soil profiles	69

Figure 5.17	Variation of stress XY in time domain for various soil profiles	71

Figure 5.18	Variation of strain XX in time domain for various soil profiles	73

Figure 5.19	Variation of strain YY in time domain for various soil profiles	75

Figure 5.20	Variation of strain XY in time domain for various soil profiles	77

##### List of Symbols used

		Shear strain

		Shear stress

		Shear strain at turning point

		Shear stress at turning point

Go		Initial shear modulus

Eo		Initial elastic normal modulus

		Poisson’s ratio

N		Corrected standard penetration test value

Vs		Shear velocity

fck		Uniaxial compressive strength of concrete

fc’		Uniaxial compressive strength of concrete

ft		Tensile strength of concrete

fy		Yield strength of steel

Kn		Spring constant for normal spring

Ks		Spring constant for shear spring

n		Normal stress

		Normal strain

y		Shear stress

I1		First strain invariant

I		Mean inelastic strain

##### List of Abbreviations used

RC		Reinforced Concrete

FEM		Finite Element Method

PGA		Peak Ground Acceleration

FE		Finite Element

2D		Two Dimensional

SPT		Standard Penetration Test

UG		Underground